# Calcium Aluminate Cement (Bmpr)

Effective:  July 1, 2013

Revise Article 1001.01(e) to read:

“(e)	Calcium Aluminate Cement.  Calcium aluminate cement shall be used according to Article 1020.04 or when approved by the Engineer.  The cement shall meet the standard physical requirements for Type I cement according to AASHTO M 85, except the time of setting shall not apply.  The chemical requirements shall be determined according to AASHTO T 105 and shall be as follows: minimum 37 percent aluminum oxide (Al2O3), maximum 42 percent calcium oxide (CaO), maximum 1 percent magnesium oxide (MgO), maximum 0.4 percent sulfur trioxide (SO3), maximum 1.75 percent loss on ignition, and maximum 7 percent insoluble residue.”